




Mapejoint 100/12
[bookmark: _GoBack]Supply and application of prefabricated polymer composite jointing strip (such as Mapejoint 100/12 by MAPEI S.p.A.), suitable for reconstructing and protecting damaged joints and withstanding medium amounts of movement, highly resistant to wear caused by moving vehicles, including industrial vehicles. The prefabricated jointing strip must be bonded to the sub-layer, in a pocket created in the floor so that it straddles the joint being repaired, using high-performance epoxy adhesive with a paste consistency (such as Mapefloor JA or Mapefloor JA Fast by MAPEI S.p.A.).

	The prefabricated jointing strip must have the following characteristics:

	Dimensions (length x width x thickness):
	1000 x 120 x 25

	Compressive strength (N/mm²):
	90

	Flexural strength (N/mm²):
	75

	Maximum width of open joint (mm):
	10

	Maximum permitted horizontal movement (mm):
	5
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